Testing Recap Log

Metcalf Avenue 151st to 135th Street

KDOT Project No.: 46 N 0186-01 OP Project No.: Th-0356

| Types of tests performed | Testing frequency | Quantity Totals | # of tests performed | Actual testing Frequency | Pass/Fail | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| Fly Ash | 1 per 600m2 | 90858m2 | 61 | 1 per 1489m2 | 52/9 | See note 1. Retests passed |
| CONCRETE |  |  |  |  |  |  |
| Structures | 1 per 50m3 | 141m3 | 12 | 1 per 12m3 | 12/0 |  |
| Curb | 1 per 150m | 13721.16m | 22 | 1 per 623m | 21/1 | See note 1. Retest passed |
| Sidewalk | 1 per 500m2 | 7096.07 | 9 | 1 per 788m2 | 9/0 | See note 1. |
| Drives | 1 per 500m2 | 1879.00m2 | 3 | 1 per 626m2 | 3/0 | See notes 1 & 2. |
| GRADATION |  |  |  |  |  |  |
| OP Special | 1 per 1000t | 18459.83 | 16 | 1 per 1153t | 14/2 | Retest passed |
| Edge Drain | 1 per 250t |  | 2 |  | 2/0 | See note 3. |
| Storm Sewer and BD-1 |  |  | 4 |  | 3/1 | See note 4.Retest passed |
| Asphalt | As per Engineer | 48266.57t | 41 | 1 per 1177t | 41/0 | See note 5. |
| Compaction of Soils | 1 per 600m2 | 56752m3 | 61 | 1 per 930m3 | 49/12 | See note 6. |

Notes:

- Tested at beginning of daily run and as needed there after.

- Most drives poured at same time as curb.

- Tested per phase, most delivered at one time for each phase.

- No specified testing frequency. Tested for assurance.

- Tested once in AM and PM or as needed.

- Tested per lift or at least twice daily.

Refer to log notes or testing reports for reasons of test failures.

Kevin J. Shaunty

Construction Inspector, Senior