Testing Recap Log

Metcalf Avenue 151st to 135th Street

KDOT Project No.: 46 N 0186-01 OP Project No.: Th-0356

Types of tests performed	Testing frequency	Quantity Totals	# of tests performed	Actual testing Frequency	Pass/Fail	Remarks
Fly Ash	1 per 600m2	90858m2	61	1 per 1489m2	52/9	See note 1. Retests passed
CONCRETE
Structures	1 per 50m3	141m3	12	1 per 12m3	12/0
Curb	1 per 150m	13721.16m	22	1 per 623m	21/1	See note 1. Retest passed
Sidewalk	1 per 500m2	7096.07	9	1 per 788m2	9/0	See note 1.
Drives	1 per 500m2	1879.00m2	3	1 per 626m2	3/0	See notes 1 & 2.
GRADATION
OP Special	1 per 1000t	18459.83	16	1 per 1153t	14/2	Retest passed
Edge Drain	1 per 250t
2
2/0	See note 3.
Storm Sewer and BD-1
4
3/1	See note 4.Retest passed
Asphalt	As per Engineer	48266.57t	41	1 per 1177t	41/0	See note 5.
Compaction of Soils	1 per 600m2	56752m3	61	1 per 930m3	49/12	See note 6.

Notes:

Tested at beginning of daily run and as needed there after.

Most drives poured at same time as curb.

Tested per phase, most delivered at one time for each phase.

No specified testing frequency. Tested for assurance.

Tested once in AM and PM or as needed.

Tested per lift or at least twice daily.

Refer to log notes or testing reports for reasons of test failures.

Kevin J. Shaunty

Construction Inspector, Senior

Material Testing Log

Kevin Shaunty

2004-05-24

Joe Archer

City of Overland Park